B-Flux 120 (Halide Flux)

EXPLANATION

B-Flux 120 (Halide Free) is a  Halide Free No clean flux, with fine wetting properties, used for both Pb free and Sn/Pb soldering applications. Specifically developed to deliver high reliability and excellent soldering performance combined with outstanding board cosmetics and pin-testability

Features:

- Halide free, which is environment friendly,

- Fine soldering in both wave soldering processes.

- Low tendency.

- Good cosmetics

- Cadmium, OSP, Tin, Copper, Gold, Zinc and Silver

Benefits:

• Environmental friendly. Complies with halogen-free industries standards

• Produces highly reliable assemblies with excellent cosmetics and pin testability

• High through-hole penetration rate and uniform SMT pad coverage

Flux Application:

B-Flux 120 can be applied by Foam, spray, Dipping, or brushing. To achieve good results, a uniform coating of flux is required on the board. Materials used shall comply with ionic cleanliness to meet electrical stability and consistent soldering performance.

OPERATING PARAMETER

| Amount of Flux Applied | Single : 1,200 to 1,600 µg/in2 solids Dual : 1,400 to 1850 µg/in2 solids |
| --- | --- |
| Top-Side Preheat Temperature | 90 - 120°C |
| Bottom side Preheat Temperature | 110 - 140°C |
| Contact Time in the Solder (includes Chip Wave and Primary Wave) | 3 – 6 seconds |
| Solder Pot Temperature | 245-255°C for 63/37, 255-265°C for Lead Free SAC alloys |

TECHNICAL DATA

| Test | SPECIFIC PARAMETERS |
| --- | --- |
| Appearance | Clear, Colourless Liquid |
| Solids Content, wt/wt | 2.0% +/- 0.1 |
| IPC-J-STD-0004 Designation | ORLO |
| Acid Number mg KOH/g | 23.5 +/- 0.5 |
| Specific gravity @ 25°C | 0.794 +/- 0.01 |
| Flash Point | 15 ֯ C |
| IPC J-STD-004 Comb- UP and Down un-Cleaned | Meets IPC, JIS for corrosion and Copper mirror tests, Bellcore Surface Insulation Resistance and Electro Migration requirements |
| Saleable | 540 Days |

### RESIDUE REMOVAL

B-Flux 120 (Hallide) is a no-clean board; flux residues are designed to be left on the board. If desired, Flux residues can be removed with a water-based cleaner i,e, B-ABC-09, solvent-based cleaners i.e B-E Friendly 100 DL, B-Cleaner 250, or IPA Electronic Grade.

### OUR PRODUCT ENCASING TYPE

Packaging is available in 5 and 20 Litres (HDPE White carboy Container)

### HEALTH AND SAF	ETY

Observe standard precautions for handling. Eye and skin protection must be provided. Avoid breathing of liquid. For detailed information refer to the relevant Health and Safety Data Sheet (MSDS) available on request.